BATCH MANUFACTURING RECORD

Lube Oil Blending Plant — Engine Oil 15W-40 API SN

Document No: BMR-15W40-2024-08417  |  Revision: 1.0  |  Date: 12-Aug-2024

## 1. Batch Header Information

| Parameter | Value | Remarks |
| --- | --- | --- |
| Process Order | PO-2024-08417 | SAP PP-PI |
| Product Grade | LOBP-15W40-API-SN | Lubricant type: Engine Oil |
| Batch Number | B-2024-08417-01 | Auto-generated by SAP |
| Batch Size Target | 20,000 Litres | ±2% tolerance |
| Blending Vessel | V-102 (Atmospheric Blender) | Capacity: 25,000 L |
| Planned Start | 12-Aug-2024 06:00 | Night shift handover |
| Planned End | 12-Aug-2024 14:00 | Day shift completion |
| Formula Version | FM-15W40-SN-v3.2 | Approved QC: 04-Jun-2024 |

## 2. Formula & Ingredient Dispensing Log

All quantities verified by operator and cross-checked against SAP process order. Raw materials dispensed from approved lots only.

| Ingredient | Type | Material Code | Volume (L) | UOM | Batch % | Lot No. |
| --- | --- | --- | --- | --- | --- | --- |
| Base Oil SN-150 | API Group I | BO-SN150-SHELL | 12,400 | L | 60.9% | LOT-2024001 |
| Base Oil SN-500 | API Group I | BO-SN500-SHELL | 3,600 | L | 17.7% | LOT-2024018 |
| Viscosity Index Improver | OCP Polymer | ADD-VII-LUBRIZOL | 1,200 | L | 5.9% | LOT-2024035 |
| ZDDP Antiwear Package | Zinc-Phosphorus | ADD-ZDDP-AFTON | 1,000 | L | 4.9% | LOT-2024052 |
| Detergent/Dispersant Pack | Ca Sulphonate | ADD-DD-INFINEUM | 1,440 | L | 7.1% | LOT-2024069 |
| Pour Point Depressant | Polymethacrylate | ADD-PPD-EVONIK | 160 | L | 0.8% | LOT-2024086 |
| Anti-foam Additive | Silicone-based | ADD-AF-DOW | 8 | L | 0.04% | LOT-2024103 |
| Dye (Blue Marker) | Solvent Blue 35 | ADD-DYE-BLUE | 12 | L | 0.06% | LOT-2024120 |

## 3. Blending Process Log

| Step | Time | Operator | Action / Reading |
| --- | --- | --- | --- |
| Step 1 — Pre-heat BO | 06:15 | Rajan K. | Base oil SN-150 heated to 55°C. Agitator started at 60 RPM. Tank temp confirmed on DCS tag V102-TI-01. |
| Step 2 — BO Transfer | 06:45 | Rajan K. | SN-150 transferred via P-201 pump. Flow meter totaliser: 12,400 L confirmed. |
| Step 3 — BO Blend | 07:10 | Rajan K. | SN-500 added. Agitator increased to 80 RPM. Blend temp 58°C. |
| Step 4 — Additive Addition | 07:45 | Priya M. | Additives added in sequence: ZDDP → DD Pack → VII → PPD → AF → Dye. Each confirmed by weight. |
| Step 5 — Homogenisation | 08:30 | Priya M. | Full blend at 80 RPM, 60°C for 90 minutes. Viscosity grab sample taken at 10:00. |
| Step 6 — QC Hold Sample | 10:05 | Suresh V. | 1-litre sample drawn from bottom drain point. Sent to LIMS with sample ID SMP-08417-01. |
| Step 7 — QC Approval | 11:45 | QC Lab | All parameters PASS. Usage decision entered in SAP QM. Batch released. |
| Step 8 — Transfer to FG | 12:30 | Rajan K. | Finished product transferred to FG Tank T-08 via P-301. 19,940 L received (yield: 99.7%). |

## 4. In-Process & Final QC Results

| Test Parameter | Method | Specification | Result | Status |
| --- | --- | --- | --- | --- |
| Kinematic Viscosity @100°C | ASTM D445 | 12.5–16.3 cSt | 14.2 cSt | PASS |
| Kinematic Viscosity @40°C | ASTM D445 | 109–125 cSt | 116.8 cSt | PASS |
| Viscosity Index | ASTM D2270 | ≥120 | 138 | PASS |
| Flash Point (COC) | ASTM D92 | ≥220°C | 234°C | PASS |
| Pour Point | ASTM D97 | ≤ −18°C | −24°C | PASS |
| Total Base Number | ASTM D2896 | ≥8.0 mg KOH/g | 9.4 mg KOH/g | PASS |
| Sulphated Ash | ASTM D874 | ≤1.2 wt% | 0.98 wt% | PASS |
| Zinc Content | ASTM D5185 | ≥900 ppm | 1,024 ppm | PASS |
| Phosphorus Content | ASTM D5185 | ≥800 ppm | 912 ppm | PASS |
| Colour (ASTM) | ASTM D1500 | ≤3.0 | 2.5 | PASS |

## 5. Approvals & Sign-Off

| Role | Name | Signature | Date/Time |
| --- | --- | --- | --- |
| Blending Operator | Rajan Kumar | Signed | 12-Aug-2024 12:30 |
| QC Analyst | Priya Mehta | Signed | 12-Aug-2024 11:45 |
| Shift Supervisor | Suresh Venkataraman | Signed | 12-Aug-2024 12:45 |
| QC Manager | Dr. Anitha Rao | Signed | 12-Aug-2024 13:00 |

This Batch Manufacturing Record is generated from SAP PP-PI Process Order PO-2024-08417 and is the controlled master record for batch B-2024-08417-01. Physical copy retained in batch file. Digital record archived in SAP DMS.