QUALITY CONTROL TEST PROCEDURES

& FINISHED PRODUCT SPECIFICATIONS

Document No: QC-SPEC-001  |  Rev 3.0  |  Approved by: Dr. Anitha Rao (QC Manager)  |  Date: 01-Jan-2024

# 1. Finished Product Specification Matrix

All specifications are mandatory. Products failing any parameter are placed on QC Hold in SAP QM and must not be transferred to Finished Goods storage. Retesting is permitted once; a second failure triggers Non-Conformance Report (NCR) procedure QC-NCR-001.

| Product Grade | SAP Material | Test Method | KV @100°C | KV @40°C | HTHS @150°C | VI Min | Flash Pt Min | Pour Pt Max | TBN/TAN | Sulph. Ash Max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Engine Oil 15W-40 API SN | EO-15W40-SN | ASTM D445 | 12.5–16.3 cSt | 109–125 cSt | — | ≥120 | ≥220°C | ≤ −18°C | ≥8.0 | ≤1.2 |
| Engine Oil 20W-50 API CF | EO-20W50-CF | ASTM D445 | 16.3–21.9 cSt | 150–185 cSt | — | ≥90 | ≥230°C | ≤ −15°C | ≥7.0 | ≤1.5 |
| Hydraulic Oil ISO 46 | HO-ISO46 | ASTM D445 | 41.4–50.6 cSt | — | — | ≥95 | ≥180°C | ≤ −27°C | ≥1.0 (TAN) | ≤0.01 |
| Gear Oil SAE 90 | GO-SAE90 | ASTM D445 | 13.5–18.5 cSt (100°C) | — | — | — | ≥170°C | ≤ −12°C | ≥2.0 | ≤0.1 |
| Compressor Oil ISO 100 | CO-ISO100 | ASTM D445 | 90–110 cSt | — | — | ≥105 | ≥220°C | ≤ −15°C | ≤1.0 (TAN) | — |
| Turbine Oil ISO 32 | TO-ISO32 | ASTM D445 | 28.8–35.2 cSt | — | — | ≥100 | ≥170°C | ≤ −18°C | — | — |

# 2. Test Procedures — Standard Operating Procedures

## 2.1  SOP-QC-001: Kinematic Viscosity — ASTM D445

Instrument: Cannon-Fenske Routine Viscometer / Anton Paar SVM 3001 Automated Viscometer

Temperature Bath: ±0.01°C stability required. Calibrate daily with certified standard oils.

Reference Standard: Cannon Certified Viscosity Standard — S3 (nominal 3 cSt) and N100 (nominal 100 cSt)

| Step | Procedure | Acceptance / Record |
| --- | --- | --- |
| 1 | Bring sample to room temperature (23±2°C). Gently invert sample bottle 10 times to ensure homogeneity. Do not shake. | Sample temperature confirmed. Homogeneity visual check: no cloudiness or separation. |
| 2 | Select correct viscometer tube size per ASTM D446 selection table based on expected viscosity range. Clean tube with petroleum naphtha, then acetone, blow dry with filtered air. | Tube size recorded in LIMS. No moisture visible after drying. |
| 3 | Fill viscometer to lower fill mark. Place in bath at 40°C or 100°C as required. Allow 30-minute equilibration. | Bath temperature logged from calibrated thermometer. Equilibration time confirmed. |
| 4 | Apply suction to bring oil to upper timing mark. Release suction. Record time (in seconds) for oil meniscus to travel from upper to lower timing mark. Perform duplicate runs. | Two runs within 0.35% of each other (ASTM D445 repeatability limit). If not, repeat. |
| 5 | Calculate KV: KV (cSt) = C × t, where C = viscometer constant (from certificate) and t = mean flow time (s). | Result entered in LIMS. Auto-compare to specification. Flag if out of spec. |
| 6 | Calculate Viscosity Index (ASTM D2270) if both @40°C and @100°C results are available. | VI calculated by LIMS automatically from paired results. |

## 2.2  SOP-QC-002: Flash Point — ASTM D92 (Cleveland Open Cup)

Instrument: Cleveland Open Cup Apparatus with automated flame applicator (Koehler K16300)

Calibration: Verify with certified oil standard. Record ambient temperature and barometric pressure.

| Step | Procedure | Acceptance / Record |
| --- | --- | --- |
| 1 | Fill COC cup to the fill line (no more). Heat at 14–17°C/min up to 56°C below expected flash point, then slow to 5–6°C/min. | Heating rate verified by thermocouple readout. Recorded in LIMS. |
| 2 | Apply test flame (4 mm diameter) in a sweep across the cup every 2°C. First flash is confirmed by a distinct blue halo — not the flame enlarging. | Flash point = temperature at first confirmed flash. Barometric correction: FP(corrected) = FP(obs) + 0.25×(101.3 − P_atm). |
| 3 | Continue heating to fire point (sustained burn ≥5 seconds). Record both flash and fire points. | Both values entered in LIMS. Fire point normally 25–30°C above flash point. |

## 2.3  SOP-QC-003: Total Base Number (TBN) — ASTM D2896

TBN measures the alkalinity reserve of engine oils, indicating their ability to neutralise acidic combustion by-products. It is expressed as mg KOH/g.

Instrument: Metrohm 916 Ti-Touch Autotitrator with HClO4 titrant in acetic acid

- Weigh 1.0 g ±0.001 g of sample into titration vessel. Add 60 mL chlorobenzene:glacial acetic acid (1:1 v/v) solvent.

- Standardise HClO4 titrant against KH-phthalate before each batch of samples.

- Titrate to potentiometric inflection point. Calculate: TBN = (V_sample − V_blank) × N × 56,100 / W_sample

- Units: mg KOH/g. LIMS auto-calculates from titrant volume, normality, and sample weight inputs.

Repeatability limit (ASTM D2896): ±0.5% of mean for TBN >10 mg KOH/g. If duplicate results exceed this, reject and retest.

# 3. Non-Conformance Procedure

When any parameter fails specification: (1) Place batch on QC Hold in SAP QM immediately. (2) Notify QC Manager and Production Supervisor within 30 minutes. (3) Raise Non-Conformance Report (NCR) in LIMS within 2 hours. (4) Root cause investigation within 24 hours. (5) Corrective action plan approved by QC Manager before any rework or disposal decision.

Rework: Permitted once per batch, for viscosity and additive-related failures only. Re-test all parameters after rework.

Disposal: If rework not viable: segregate, label 'OFF-SPEC — DO NOT SHIP', and dispose per MSDS/SDS hazardous waste procedure.